DECO APPLICATION GUIDELINE

DECO 20 Concrete Clear

Block Wall - Exterior

Ensure surface is clean and dry. Surface of mortar should be dry before applying Deco 20.  If wall is parged meaning a concrete slurry mix is applied over the block the concrete mix surface should be dry first. Dryer the better.

Best to apply with temps between 32+ and lower than 95 degrees. Hot days best to apply on mornings.

Apply liberal coat of Deco 20 to allow material to thoroughly soak block & mortar. No run downs req’d.

Apply above & below grade also footer joint and on footer. Clean footer w/ broom before applying.

Any remaining Deco 20 can be applied on interior wall or flat surfaces such as floor pads, sidewalks, etc.

Deco 20 is paintable, colorless, odorless, safe to apply w/ any sprayer. Only 1 coat required.

Cure/Dry time is approx. 4-6 hours depending on temp, humidity, porosity.

DO NOT APPLY with threat of rain in forecast.

Block Wall - Interior

Ensure surface is clean and dry as possible. Remove paint or efflorescence w/ wire brush and dust broom.

If wall is damp install fans, open windows to dry wall best you can. Dryer the wall more Deco 20 enters.

Fill any wide cracks that are visually apparent w/ concrete or hydraulic mix before applying Deco 20.

Apply liberal coat of Deco 20 to allow material to thoroughly soak block & mortar. No run downs req’d.

Apply above & below grade also footer joint and on footer. Clean footer w/ broom before applying.

See Above Italic line items on misc. questions.

Precast or Poured Concrete Wall

On new poured wall wait 1 full day after forms are removed for form oil/release agent to dissipate.

Best to fill wall tie voids & honeycombing w/ Deco Tie Patch. Let Tie Patch dry first before apply Deco 20.

Best to apply with temps between 32+ and lower than 95 degrees. Hot days best to apply on mornings.

Apply liberal coat of Deco 20 to allow material to thoroughly soak wall. No run downs req’d.

Apply above & below grade also footer joint and on footer. Clean footer w/ broom before applying.

See above Italic line items on Misc. questions.

Flatwork

Ensure all cracks on concrete are filled w/ cement or hydraulic mix and surface is clean and dry.

Apply on porous surfaces of concrete driveway, sidewalks, patios, etc.

Do Not Apply on non-porous surfaces such as stamped concrete. Deco 20 will not penetrate/work.

Apply liberal coat of Deco 20 to concrete. Do not let product puddle on surface face, broom out puddles.

Only 1 coat required

DECO TIE PATCH

Designed to fill any concrete wall voids, large cracks, openings and honeycombing.

Surface to be clean and dry before applying Tie Patch. A spackle knife works best to fill patch into concrete.

Larger openings may require second application of Tie Patch.

Let Tie Patch dry before applying Deco 20. Tie Patch can be wet/damp if applying Deco Seal or Dampproof coating.

Water based, odorless, safe to apply, paintable. No not apply with threat of rain in forecast.

OVER….

DECO SEAL

Block Wall - Exterior

Ensure surface is clean and dry. Surface of mortar should be dry at the surface before applying Seal.

If wall is parged (concrete slurry mix over block) the concrete mix surface should be dry first.

If wall is NOT parged you must apply 1 coat of DECO 20 which acts as primer first. Let Deco 20 dry then apply Seal.

You can spray, roll or brush on Seal.  Stir well before applying.

Use a 3/4” or 1” nap roller which allows more Seal to go on roller. A short handle 4” masonry brush is fine.

Sprayer Specs – Must have flow rate of 1-2 gallons per minute AND provide 2500 PSI output.

Typical airless sprayers or rental sprayers are designed for paint not for Deco Seal or elastomeric coatings.

Spray one coat on wall liberally. Do not allow product to run down off wall it’s too thick/heavy if running down.

Continue spraying entire wall then go back and spray second thin coat on wall with no rundowns. If first coat is too wet or hasn’t dried enough you may have to wait 1-2 hours before applying second coat. The advantage of spraying you don’t have to wait for first coat to completely dry. Spray footer joint where block sets on footer. Spray heavy into this joint & let it fill in fully. Footer can be sprayed.

Roll or Brush On – Apply one coat on wall liberally but do not allow product to run down off wall.  It’s best to wait for first coat to be dry before applying second coat.  Use paint or masonry brush to apply Seal in footer joint.

Footer Joint – Weakest part of your wall. Get as much Seal into this joint. Can apply on footer but clean first.

Protection Board – optional but if grade is rocky, shale, not clean or heavy clay we recommend ½” to 1” pink/blue board 4’x8’ sheets. Apply Liquid Nails on boards then on wall onto dry Deco Seal.

Can be applied Above & Below grade. Odorless, UV Resistant, Tan or Gray Color, it’s paintable, waterbased, non-hazard

Cure/Dry time is approx. 8-12 hours for each coat depending on temp, humidity, porosity.

DO NOT APPLY with threat of rain in forecast and temperature to be 28 degrees and rising or above.

Block Wall - Interior

Not designed for interior walls. If walls are damp apply Deco 20 clear. If walls are wet or have water entering wall do not try to fix from interior. Call DecoSealers if water is entering wall(s).

Precast or Poured Concrete Wall

Best to fill wall tie voids & honeycombing w/ Deco Tie Patch. Let Tie Patch dry first before apply Seal.

Can apply Seal as soon as forms are removed.

See Instructions Above regarding spraying, rolling or brushing Seal on wall.

See Italic above instructions

DECO TAC

Designed to be applied over old foundation wall coating to provide strong adhesion to new foundation wall coating

Clean existing tar, foundation coating, dirt off wall. Clean and dry is always best.  Apply w/ roller or brush only.

Pour TAC into paint pan and apply thin coat onto wall. TAC will be milky white when applying.

In approx. 30-45 minutes TAC will turn clear and then you have a 6-8 hour window to apply new foundation coating. If you have a large application best to apply TAC in phases.

Water based, non-hazardous, very low odor, easy clean up, do not apply with threat of rain in forecast.

ANY FURTHER QUESTIONS THAT AREN’T LISTED

PLEASE CALL DECOSEALERS: 717.484.6131