DECO APPLICATION GUIDELINE

DECO 20 Concrete Clear Sealer

(do not get on glass, black roof or driveways – see container label for further details)

Block Wall - Exterior

Ensure surface is clean and dry. Surface of mortar should be dry before applying Deco 20.  If wall is parged meaning a concrete slurry mix or mortar coat applied over the block this parge surface should be dry first.

Best to apply with temps between 32+ and lower than 95 degrees. Hot days best to apply on mornings/evening.

Apply flood coat of Deco 20 to allow material to thoroughly soak block & mortar. Allow run downs.

Apply above & below grade including footer joint and on footer. Clean footer w/ broom before applying.

Any remaining Deco 20 can be applied on interior wall or flat porous surfaces such as patios, sidewalks, etc.

Deco 20 is paintable, colorless, odorless, safe to apply w/ any sprayer. Only 1 coat required.

Cure/Dry time is approx. 2-4 hours depending on temp, humidity, porosity.

DO NOT APPLY with threat of rain in forecast.

Block Wall - Interior

Ensure surface is clean and dry as possible. Remove paint or efflorescence w/ wire brush and dust broom.

If wall is damp install fans, open windows to dry wall. The dryer the wall more it will take Deco 20 .

Fill any wide cracks that are visually apparent w/ Deco Tie Patch or hydraulic mix before applying Deco 20.

Apply flood coat of Deco 20 to allow material to thoroughly soak block & mortar.

See Above Italic line items on misc. questions.

Precast or Poured Concrete Wall

On new poured wall wait 1 full day after forms are removed for form oil/release agent to dissipate.

Best to fill wall tie voids & honeycombing w/ Deco Tie Patch. Let Tie Patch dry first before apply Deco 20.

Best to apply with temps between 32+ and lower than 95 degrees. Hot days best to apply on mornings.

Apply flood coat of Deco 20 to allow material to thoroughly soak wall.

Apply above & below grade also footer joint and on footer. Clean footer w/ broom before applying.

See above Italic line items on Misc. questions.

Flatwork/Sidewalks/Patios/Driveways

Ensure all cracks on concrete are filled w/ cement or hydraulic mix and surface is clean and dry.

Apply on porous surfaces of concrete driveway, sidewalks, patios, etc. Only 1 coat required

Do Not Apply on non-porous surfaces such as stamped concrete. Deco 20 will not penetrate/work.

Apply flood coat of Deco 20 to concrete. Do not let product puddle on surface face, broom out puddles.

DECO Tie Patch

- Designed to fill any concrete wall voids, small cracks, openings and light honeycombing.

- Surface to be clean and dry before applying Tie Patch. A spackle knife or your hand w/ gloves works best to fill patch into concrete. **Remove all rust w/ wire brush if present, clean w/ rag before applying Patch.

- Larger openings may require second application of Tie Patch. Tie Patch is not quick setting. Hydraulic Cement (HC) is a good alternative for cracks or holes larger than ¼”. Down side to HC it cracks in time.

- Let Tie Patch dry before applying Deco 20 Seal. Tie Patch can be wet/damp when applying Deco 20 Seal or Dampproof coating over it. Ideally it’s best for Tie Patch to be dry before applying Seal over it.

- Water based, odorless, safe to apply, paintable. Do not apply with threat of rain in forecast.

OVER….

DECO 20 SEAL Waterproofing Membrane & Dampproofing Coating

Precast or Poured Concrete Wall

- Wait one day or more after forms come off wall. This allows form oil or release agent to dissipate. In addition, the wall is trying to cure so it’s helpful to allow moisture in concrete wall to escape. Ideally 2-3 days is best min. option to apply Seal.

- Best to fill wall tie voids, cracks larger than hairline & honeycombing w/ Deco Tie Patch the next day or later when forms are removed. Applying the patch a day or more before Seal applic., allows it to cure.

- It’s best if Tie Patch dries first before applying Seal. But if scheduling is tight you can apply SEAL over damp Tie Patch. See Tie Patch section on opposite page for further details.

- If Deco 20 SEAL sits for a week or more after shipment it’s best to mix SEAL thoroughly bc the high quality resins want to drop to the bottom of bucket & brings water to the top. Use Drill mixer/strong paint stick.

Block Wall – Exterior Only (not designed for interior wall)

Ensure surface is clean and dry. Surface of mortar should be dry at the surface before applying Seal.

If wall is parged (concrete slurry mix or mortar coat over block) the concrete mix surface should be dry first.

A non-parged wall you must spray 1 coat of DECO 20 Clear as a primer first. Let Deco 20 Clear dry then apply Seal.

Sprayer Specs – Must have flow rate of 1-2 gallons per minute AND provide 2500 PSI output.

Typical airless sprayers or rental sprayers are designed for paint not for Deco 20Seal or elastomeric coatings. Refer to a Graco 5900 or 7900 sprayer spec’s. These types of sprayers are designed for SEAL. Use a 531 or 631 spray tip.

Application Instructions

Sprayer – A typical airless sprayer will not work. See sprayer Specs. Above.  Apply one coat on wall liberally. Do not allow product to run down off wall – that’s too thick.

Continue spraying entire wall then go back and spray second thin coat on wall with no rundowns. If first coat is too wet or hasn’t dried enough you may have to wait 2-4 hours before applying second coat. The advantage of spraying you don’t have to wait for first coat to completely dry. Spray footer joint where block sets on footer. Spray heavy into this joint & let it fill in fully.  Roll or Brush On – Most common method…Apply one coat on wall liberally but do not allow product to run down off wall.  Best to wait for first coat to dry before applying second coat. 8-12hrs typical cure time before second coat. Use a 3/4” or 1” nap roller vs. 3/8” roller which allows more Seal to go on roller. A short handle brush is fine but roller provides higher coverage rate. Use brush to apply Seal in footer joint.

Footer Joint – Weakest part of your wall. Apply heavy coat into this joint.    Optional: Apply Seal on top of footer.

Protection Boards – optional, if grade is rocky, shale, not clean or heavy clay we recommend 1” white foam board 4’x8’ sheets. Pink/Blue boards are fine but more expensive. Sharp edges/rocks can scratch the Seal when backfilling. Boards are just for protection when backfilling not part of waterproof system. Depending on your grade line you can turn the sheets sideways so 4’ is your height & 8’ width. The bottom 3’-5’ is the most critical area regarding hydrostatic water pressure. Apply Liquid Nails or an adhesive on one side of board then apply on wall onto our dry Deco Seal.

Can be applied Above & Below grade. Odorless, UV Resistant, Biege or Gray Color, it’s paintable, waterbased, non-hazard. Cure/Dry time is approx. 8-12 hours for each coat depending on temp, humidity, porosity.

DO NOT APPLY with threat of rain in forecast and temperature to be 28 degrees and rising or above to apply.

DECO TAC – Adhesive Primer

- Apply over old foundation wall coating/existing backfilled walls to provide strong adhesion for Deco 20 Seal

- Clean existing tar, foundation coating, dirt off wall. Clean and dry is always best.  Apply TAC w/ roller or brush only.

- Pour TAC into paint pan and apply thin coat onto wall. TAC will be milky white when applying.

- In approx. 30-45 minutes TAC will turn clear and then you have a 6-8 hour window to apply Deco 20 Seal.

- If you have a large application best to apply TAC in phases. Do not leave TAC exposed overnite w/o Seal.

- Water based, non-hazardous, very low odor, easy clean up, do not apply with threat of rain in forecast.

ANY FURTHER QUESTIONS THAT AREN’T LISTED

PLEASE CALL DECOSEALERS: 717.484.6131